**Product description**

**Sheet (**This series is also commonly known as **Kang-Pao)**

**Applicable products**

* All kinds of footwear men's shoes, women's shoes, sports shoes ...
* Cloth can be produced in accordance with demand.

**Operation method**

* Suitable solvents are toluene, acetone, methyl ethyl ketone, dichloromethane can play bridging function.
* Can be directly dip the solvent use, can also be used after the brush dip the solvent cleaning Kang-Pao, both can be the best adhesion and hardening effect.
* If you want to paste on the heel with the skin, the application of adhesive can use L-ATEX or yellow paste.

**Company code**

|  |  |  |
| --- | --- | --- |
|  | thickness | width |
| CP-605A | 0.4mm$\pm $0.05mm | 36” or more |
| CP-607A | 0.7mm$\pm $0.1mm | 36” or more |
| CP-611A | 1.1mm$\pm $0.1mm | 36” or more |
| Production thickness  | 0.5~1.1 mm | Use: Fine cloth |

|  |  |  |
| --- | --- | --- |
|  | thickness | width |
| CP-605 | 0.5mm$\pm $0.05mm | 36” or more |
| Production thickness | 0.5 | Use: Lining |

|  |  |  |
| --- | --- | --- |
|  | thickness | width |
| CP-607T/R | 0.5mm$\pm $0.05mm | 36” or more |
| CP-608T/R | 0.8mm$\pm $0.1mm | 36” or more |
| CP-630T/R | 3.0mm$\pm $0.1mm | 36” or more |
| Production thickness | 0.6~3.0 mm | Use: Non-woven fabric |