**Product Description**

**Hot - melt adhesives**

**Applicable products**

* Apply to all kinds of footwear toe sheet , counter, hats ... , the need for stereotypes of the product.
* Cloth can be produced in accordance with demand.

**Operation method**

* can be directly stitched in the upper of the counter.
* White paste or yellow paste can be rubbed on any side of the product, you can be fixed to the upper.
* Applicable to all stereotypes of the heel shoes, the temperature is recommended for more than 150 degrees Celsius, time 30 to 40 seconds.
* Applicable temperature can be specified for manufacturing.

**Company code**

* **S means single-sided adhesive**
* **W means double-sided adhesive**

|  |  |  |
| --- | --- | --- |
|  | thickness | width |
| CP-04S | 0.4mm$\pm $0.05mm | 36” or more |
| CP-04W | 0.4mm$\pm $0.05mm | 36” or more |
| CP-08S | 0.8mm$\pm $0.1mm | 36” or more |
| CP-08W | 0.8mm$\pm $0.1mm | 36” or more |
| CP-12S | 1.2mm$\pm $0.1mm | 36” or more |
| CP-12W | 1.2mm$\pm $0.1mm | 36” or more |
| Production thickness  | 0.4~1.2mm | Use: Fine cloth |

|  |  |  |
| --- | --- | --- |
| T/R-class | thickness | width |
| CP-06S T/R | 0.6mm$\pm $0.05mm | 36” or more |
| CP-06W T/R | 0.6mm$\pm $0.05mm | 36” or more |
| CP-08S T/R | 0.8mm$\pm $0.1mm | 36” or more |
| CP-08W T/R | 0.8mm$\pm $0.1mm | 36” or more |
| CP-30S T/R | 3.0mm$\pm $0.1mm | 36” or more |
| CP-30W T/R | 3.0mm$\pm $0.1mm | 36” or more |
| Production thickness | 0.6~3.0 mm | Use: Non-woven fabric |