**Product Description**

**Medium temperature hot melt adhesive “P/H/LH class”**

**Features**

* This product is composed of saturated non-woven fabric and polymer resin, is a lightweight shoe last material, and have excellent adhesion.
* P-class materials can provide good resilience and durability.
* In addition, the use of P-class materials and no additional equipment. At the same time, it and the general hot-melt film, repeatable operation.

**Company code**

* **S means single-sided adhesive**
* **W means double-sided adhesive**

|  |  |  |
| --- | --- | --- |
| P-class | thickness | width |
| CP-P08S | 0.8mm$\pm 0.1$mm | 36” or more |
| CP-P08W | 0.8mm$\pm 0.1$mm | 36” or more |
| CP-P25S | 2.5mm$\pm $0.1mm | 36” or more |
| CP-P25W | 2.5mm$\pm $0.1mm | 36” or more |
| Production thickness  | 0.8~2.5mm | Use: Non-woven fabric |
| * This series of stereotypes temperature recommended **130 ~ 140** degrees Celsius time **30** to **40** seconds.
* This series of **0.8 ~ 1.3**mm for men's, women's, children's shoes.
* This series **1.5 ~ 1.8**mm apply to all kinds of sports shoes
* This series **2.0 ~ 2.5**mm apply to all kinds of boots, skates.
 |

|  |  |  |
| --- | --- | --- |
| H-class | thickness | width |
| CP-H06S | 0.6mm$\pm $0.05mm | 36” or more |
| CP-H06W | 0.6mm$\pm $0.05mm | 36” or more |
| CP-H25S | 2.5mm$\pm $0.1mm | 36” or more |
| CP-H25W | 2.5mm$\pm $0.1mm | 36” or more |
| Production thickness  | 0.6~2.5 mm | Use: Non-woven fabric |
| * This series of stereotypes temperature recommended **130 ~ 140** degrees Celsius time **30** to **40** seconds.
* This series of **0.8 ~ 1.3**mm for men's, women's, children's shoes.
* This series **1.5 ~ 1.8**mm applies to all kinds of sports shoes.
* This series **2.0 ~ 2.5**mm applies to all kinds of boots, skates.
 |

|  |  |  |
| --- | --- | --- |
| LH-class | thickness | width |
| CP-LH08S | 0.8mm$\pm $0.05mm | 36” or more |
| CP-LH08W | 0.8mm$\pm $0.05mm | 36” or more |
| CP-LH25S | 2.5mm$\pm $0.1mm | 36” or more |
| CP-LH25W | 2.5mm$\pm $0.1mm | 36” or more |
| Production thickness  | 0.8~2.5 mm | Use: Non-woven fabric |
| * This series of stereotypes temperature recommended **130 ~ 140** degrees Celsius time **30** to **40** seconds.
* This series of **0.8 ~ 1.3**mm for men's, women's, children's shoes.
* This series **1.5 ~ 1.8**mm applies to all kinds of sports shoes.
* This series **2.0 ~ 2.5**mm applies to all kinds of boots, skates.
 |

In response to the diversification of shoes, as well as increasingly complex, rich sense of the design of the shoes, we also introduced different kinds of cloth products to meet the different needs of the client.

* **Cloth can be produced in accordance with demand.**

**Lining series :** 04PE、06PE、08PE、10PE

**Fine cloth series :** C04S、C06S、C08S、C10S、C12S

**Spunlace non - woven series :** C04PE(SK)、C06PE(SK)、C10PE(SK)

**Non-woven fabric series :** C06PE、C08PE、C10PE、C12PE、C15PE

**Stitch-bond non – woven fabric series :** C04T/RS、C06T/RS、C08T/RS、C10T/RS、C12T/RS